Detection of the sparkle texture effect by visual assessments

Omar Gómez (omar.gomez@ua.es)

Color and Vision Group, Department of Optics, Pharmacology and Anatomy,

University of Alicante, Alicante, Spain

Esther Perales (esther.perales@ua.es)

Color and Vision Group, Department of Optics, Pharmacology and Anatomy,

University of Alicante, Alicante, Spain

Elísabet Chorro (elisabet.chorro@ua.es)

Color and Vision Group, Department of Optics, Pharmacology and Anatomy,

University of Alicante, Alicante, Spain

Valentín Viqueira (valentin.viqueira@ua.es)

Color and Vision Group, Department of Optics, Pharmacology and Anatomy,

University of Alicante, Alicante, Spain

Francisco M. Martínez Verdú (verdu@ua.es)

Color and Vision Group, Department of Optics, Pharmacology and Anatomy,

University of Alicante, Alicante, Spain

In an effort to create more dynamic looking automobiles, there is an ever increasing trend among automobile manufacturers towards the use of metallic coatings in the finish of a vehicle. These coatings consist of transparent colorants mixed with metallic flakes. The flakes in the coating cause a change in color and brightness of the finish with viewing and illumination direction. This change in appearance accentuates the curves of a car, making it visually more attractive. Besides this angular dependence on viewing/illumination direction, the metallic finishes also exhibit a visually complex texture. Depending on the properties of the finish and the viewing and illumination conditions, the flakes exhibit a sparkle like texture [1], while the glossy clear coat may show a rough or smooth surface. As a result of these complex visual attributes, capturing the appearance and finding a perfect color match for a metallic finish is a non trivial task.

The main objective of this work is to evaluate the relationship between the special-effect pigments size, and the maximum distance which is detectable the sparkle texture effect [2]. For this, two different sets of samples with different structural features were evaluated in a lighting booth designed specifically for the experiment. The booth allows to vary the lighting conditions, the viewing geometry and the distance at which the sample is perceived.

A visual experiment was applied to evaluate the high correlation between a structural parameter (i.e. pigment size) and the visual appearance attribute related with texture (sparkle detection distance). Under some environmental conditions, as light intensity, color temperature and geometry of the light source, the sparkle detection distance was evaluated by applying the adjustment psychophysical method for two panel sets (metallic grays and blues), with known pigment sizes and colorimetry, with a small set of observers. The visual results show that a greater the pigment size, a greater the sparkle detection, but with some considerations.

In future, we will extend this method, even reinforced applying the statistical design of experiments (DOE), for understanding the relevance and interplay of structural (size, shape, concentration, orientation, etc.), environmental (illuminance level, color rendering, geometry, etc.) and colorimetric (dark vs. light background, chroma, etc.) factors on the sparkle detection distance.

Acknowledgments

Authors are grateful to EMRP for funding the project “Multidimensional reflectometry for industry”. The EMRP is jointly funded by the EMRP participating countries within EURAMET and the European Union. We would like to thank the Ministry of Economy and Competitiveness for the coordinated project “New developments in visual optics, vision and color technology” (DPI2011-30090-C02). Omar Gómez would also like to thank the Ministry of Economy and Competitiveness for his pre-doctoral fellowship grant (FPI BES-2012-053080).

References

Ferrero A., Campos J., Rabal A.M. and Pons A., (2013), A single analytical model for sparkle and graininess patterns in texture of effect coatings, Opt. Exp. 21, 26812-26819.

Kirchner E., van der Lans I., Perales E., Verdú F.M., Campos J., Ferrero A.. (2015) Visibility of Sparkle in Metallic Paints. (JOSA A, approved, on press).